## Slide 1: Final Class Review
K.G. Field1,a,
a kgfield@umich.edu
1University of Michigan

## Slide 2: Final Exam Structure
Same general format at Mid-Term
Non-cumulative, use slides as guide for topics to be covered

## Slide 3: Putting it into a visual

## Slide 4
Irradiation experiment workflow overview
Preparation of experiment campaign
Experiment design
Irradiation
Post-irradiation examination
Analysis and publication

## Slide 5: In-reactor Design
Cycle length/duty cycle (e.g. what’s my dose/year)
Power/flux stability per cycle (e.g. how stable?)
Experimental space (e.g. what’s the biggest thing I can put in it?)
In-situ monitoring/test capabilities
Spectrum, He/dpa, and/or transmutation effects
Uniformity of irradiation (e.g. axial peaking)
Acceptability of data to regulator (e.g. can ion beam data be used to build a neutron source?)
Accessibility (will changing political/economic environments impact my science?)
Operating temperature capabilities
Cost

## Slide 6: Sinks and defect reactions
Grain boundaries and voids classicly act as ___________?
  Neutral sinks
  Biased sinks
  Variable sinks
You are asked to derive the reaction rate for a platelet precipitate and get a prefactor of 4𝝅 to account for the geometry. How much confidence do you have in your answer?
  Low
  Moderate
  High

## Slide 7: Sinks and defect reactions
Which of the following defects/sinks are NOT unique to irradiated materials microstructures?
  Line dislocations
  Helium bubbles
  Radiation-induced segregation
  Dislocation loops

## Slide 8: Radiation Induced Segregation
If is positive, then A atoms will _________ to neutral defect sinks:
  Enrich
  Deplete
  Do nothing

## Slide 9: Radiation Induced Segregation
Decreasing the dose rate will __________ the peak temperature for RIS:
  Increase
  Decrease

## Slide 10: Radiation Induced Segregation
Your colleague proposes to introduce a third element in small quantities to a binary alloy that would change the vacancy migration energy of one of the primary alloying elements to reduce RIS. Is this a possible mechanism to reduce RIS?
  Yes
  No
  Depends

## Slide 11: Radiation Induced Segregation

## Slide 12
The 1995 Bond classic “Goldeneye” featured an opening scene where James Bond bungee jumping from a dam in Soviet Russia. At the time, the stunt held the world record for the tallest/longest jump. What was the total distance traveled?

## Slide 13: Dislocation loops
Dislocation loops can grow by either absorption or emission of point defects under irradiation
  True
  False

## Slide 14: Formation Energies
In the micrograph for dislocation loops, the loops with “shadow” contrast are:
  Faulted loops
  Unfaulted lops

## Slide 15: Formation Energies
When the stacking fault energy is high, faulted dislocation loops are:
  Less stable
  More stable

## Slide 16: Visualizing the energetics

## Slide 17: Void nucleation
The super saturation of vacancies,, will:
  Reduce the energy barrier for nucleation of voids
  Increase the energy barrier for nucleation of voids
  Have no significant effect on nucleation of voids
Sinks and interfaces in the material will:
  Reduce the energy barrier for nucleation of voids
  Increase the energy barrier for nucleation of voids
  Have no significant effect on nucleation of voids

## Slide 18: Design for Radiation Resistance III: High Sink Strength

## Slide 19: Design for Radiation Resistance III: High Sink Strength
L.K. Mansur & E.H. Lee, J. Nucl. Mater. 179-181(1991) 105

## Slide 20: Swelling
The bell shaped curve for swelling based on temperature is due to:
  Recombination dominating at low temperatures, and thermal emission dominating at high temperatures
  Recombination dominating at high temperatures, and thermal emission dominating at low temperatures

## Slide 21: Void growth
The following radial growth rate curve for a cavity is representative of?
  A void (no gas)
  A high gas content bubble
  A low gas content bubble

## Slide 22: Swelling
What material would be more resistant to swelling?
A
B

## Slide 23: Design for Radiation Resistance III: High Sink Strength
L.K. Mansur & E.H. Lee, J. Nucl. Mater. 179-181(1991) 105
Early research also investigated fine grained architectures for radiation resistance, but sufficiently stable nanoscale grain boundaries were not discovered
  Fine-grained materials are susceptible to radiation-enhanced grain growth
R. Yamada, S.J. Zinkle and G.P. Pells, J. Nucl. Mater. 209(1994) 191
S.J. Zinkle, Nucl. Instr. Meth. B 91(1994)234

## Slide 24: Bubbles
Gas atoms act to stabilize cavities and reduce the critical size to convert from a bubble embryo to a growing cavity.
  True
  False

## Slide 25: Bubbles
The full growth rate term can be analytically described as:
The different terms in order are:
Dose rate response, bias response, sink balance (Q), recombination response, thermal emission, gas response
Bias response, dose rate response, gas response, sink balance (Q), recombination response, thermal emission,
Bias response, gas response, sink balance (Q), recombination response, thermal emission, dose rate response,
Recombination response, bias response, sink balance (Q), dose rate response, thermal emission, gas response

## Slide 26: Effect of gas atoms on bubble nucleation + growth

## Slide 27: Quick review of void/bubble growth:
Tirr
% Swelling
Dose (dpa)
% Swelling
He/dpa
% Swelling

## Slide 28: Phase stability
Ostwald AND Inverse Ostwald ripening can be accelerated due radiation:
  True
  False

## Slide 29: Phase Transformations
The two primary mechanisms for precipitate stability under irradiation are:
  Supersaturation and dislocation density
  Recombination and diffusion
  Diffusion and ballistic effects
  Migration and formation energies

## Slide 31: Take home message
https://www.youtube.com/watch?v=F7IZZXQ89Oc
Material Parameters
Irradiation Parameters

## Slide 32: Take home message
https://www.youtube.com/watch?v=F7IZZXQ89Oc
Material Parameters
Irradiation Parameters

## Slide 33: Thank you!

## Slide 34: Questions?